## Slide 1: Silicon oxidation

## Slide 2: Silicon oxidation
Formation of silicon dioxide (SiO2) on silicon surface, in an oxidant ambient (O2, H2O).
SiO2 can also be deposited on silicon ( see other lessons)
Si + O2  SiO2 [dry oxidation]
or
Si + H2O SiO2+2H2 [wet oxidation]

## Slide 3: Why SiO2
Si is widely used in IC because it forms an excellent oxide, with a nearly defect-free interface.
Note: Silicon will oxidize in air at room T but...
Not enough energy for O2 to diffuse through SiO2 after a firs thin oxide layer is formed
Native oxide won’t grow more than 2 nm
Typical oxidation temperatures:
From 700 to 1100 °C

## Slide 4: ITRS roadmap for gate dielectrics

## Slide 5: SiO2 structure
SiO2 is grown as fused silica  amorphous with low range order
Rate of crystallization at typical process T can be neglected
Basic unit: SiO4 tetrahedra
Some O atoms are bonded to two Si atoms  bridging oxygen
O atoms bonded to a single Si atom  non bridging oxygen
Higher fraction of bridging to non bridging oxygen  higher cohesion and structural strength of SiO2 (dry ox. Have more bridging O2 than wet ox.)

## Slide 6: SiO2 structure: impurities
Substitutional impurities:
Replace silicon in the structure (network formers) which brings to the elimination (structure weakening) or formation of bridging oxygen (ex. Boron - Phosphorus)
Interstitial impurities:
Interstitial impurities (ex. Na, K) increase the amount of non bridging oxygen making the structure weaken and porous and increasing the diffusivity of other species within the glass (network modifiers)
Water in SiO2
Si:O:Si  Si:O:H+H:O:Si
Hydroxyls are generated and substitute bridging oxygen. The H bond is quite weak and can be easily removed  charged states or traps can be generated

## Slide 7: Oxidation kinetics
Silicon
SiO2
O2,H2O
Diffusion
Reaction
Si + O2  SiO2
Si + H2O SiO2+2H2
The oxidation process occurs at the Si/SiO2 interface
Demonstrated by several experiments, e.g. Oxygen isotopes profiling
Oxygen or water must diffuse through the silicon oxide to react at silicon surface

## Slide 8: Oxidation kinetics
Oxidation involves a volume expansion:
  ~46% of oxide thickness grows INTO the silicon, that is the silicon surface is “pushed” away for a 46% of the oxide thickness.
Stress can play a determinant role in oxidation kinetics

## Slide 9: LOCOS oxidation

## Slide 10: The Deal-Grove model of oxidation
Si
SiO2
Gas (stagnant layer)
Cg
Cs
Co
Ci
F1
F2
F3
Definitions:
Cg= Oxygen concentration at the end of stagnant layer
Cs= Oxygen concentration at the SiO2 surface
C0= Oxygen concentration in the oxide at the oxide surface
Ci= Oxygen concentration at the oxide/silicon interface
F1= Oxygen flux in the stagnant layer
F2=Oxygen flux in the oxide
F3=Oxygen flux in Si
x

## Slide 11: The Deal-Grove model of oxidation
Si
SiO2
Gas (stagnant layer)
Cg
Cs
Co
Ci
F1
F2
F3
x
Mass transport in gas phase
Solid state diffusion (Fick’s law)
Chemical reaction

## Slide 12: The Deal-Grove model of oxidation F1 calculation
Si
SiO2
Gas (stagnant layer)
Cg
Cs
Co
Ci
F1
F2
F3
Mass transport coefficient
From Henry’s law:
Partial pressure at oxide surface, not known experimental parameter
We introduce;
From perfect gas law
x

## Slide 13: The Deal-Grove model of oxidation Ci calculation
SiO2
Gas (stagnant layer)
Cg
Cs
Co
Ci
F1
F2
F3
Assuming no O2 is generated into the oxide.
And that the reaction rate is proportional to the oxidant concentration
Interface reaction rate constant
In steady state conditions F1=F2=F3; after some algebra
x
Si
Notes: Le approssimazioni per C1 e CO sono valide per h grande, il che in genere e’ vero…

## Slide 14: The Deal-Grove model of oxidation Ci calculation
Reaction controlled regime
Diffusion controlled regime

## Slide 15: The Deal-Grove model of oxidation Growth rate calculation
SiO2
Gas (stagnant layer)
Cg
Cs
Co
Ci
F1
F2
F3
The growth rate is nothing but the flux F3 divided by the number of oxidant molecules incorporated per unit volume of oxide grown N
Parabolic rate constant
Linear rate constant
x
Si

## Slide 16: The Deal-Grove model: fundamental equations

## Slide 17: The Deal-Grove model A and B/A
B and B/A are of course function of temperature. T dependence can be described as:
Ambient | B | B/A
Dry | C1=7.72E2 mm2hr-1 E1=1.23eV | C2=6.23E6 mm2hr-1 E1=2.0eV
Wet | C1=3.86E2 mm2hr-1 E1=0.78eV | C2=1.63E8 mm2hr-1 E2=2.05eV
Valid for (111) orientation, for (100) C2 must be divided by 1.68
B is more strictly related to diffusion  activation energies are very different between dry and wet ox.
B/A is more related to reaction at Si surface  activation energies are close to th energy needed to break Si-Si bonds.

## Slide 18: Corrections to Deal-Grove model
The Deal-Grove model does not work for thin oxides !
Massoud et al.:
No clear explanation of thin film regime yet:
O2- coupled diffusion
Thermoionic emission of electrons from Si into SiO2
Micro-pores
Blocking layers
Additional Si layers participating to oxidation
Deal-Grove term

## Slide 19: Oxidation rate and substrate doping
The substrate doping profile will change during oxidation, depending on impurities diffusivity and segregation coefficient (m).
m<1 for Boron
m~10 for P,As,Sb

## Slide 20: Oxidation rate and crystal orientation
B does not depend on crystal orientation
B/A strongly depends on it
Why?
  Number of Si bonds available for cm-2
  Orientation dependent stress in some cases (?)
Inverted trend for thin oxides at low O2 pressure and high pressure H2O grown oxides

## Slide 21: 2D oxidation
Parameters to be kept into account when studying 2D oxidation:
  Effects of crystal orientation on oxidation rate
  Dependence of oxidant diffusion on local shape
  Viscous flow
  Stress effects
In a classical paper (see references) Kao et al. studied oxidation rates as a function of radius of curvature of different structures

## Slide 22: Microscopic model for oxidation
Oxidation processes “consume” vacancies and produce interstitial.
  Part of the volume expansion can be modeled by vacancies consumption.
  Interstitial injection can explain dopant diffusion phenomena (OED, ORD) and extended defects formation (Oxidation-induced Stacking Faults, OSF)
Notes: e’ il numero di interstiziali per atomo di ossigeno che prendono parte alla reazione, b e’ lo stesso numero per le vacanze.

## Slide 23: Oxidation rate and substrate doping
All kinds of substrate doping increase oxidation rate
B is incorporated into SiO2 and weakens the oxide structure
Oxidant diffusion is thus enhanced
P doping shows a huge increase of B/A
Probably Ef shift increases vacancy concentration  more oxidation sites available.

## Slide 24: Charge in SiO2
Si/SiO2 defects: 109-1011 cm-2
Si surface atoms 1015 cm-2
4 main kinds of defects:
Qf= fixed oxide charge
  A sheet of positive charge close to the interface (2nm).
  Believed to be formed of incompletely oxidized Si atoms
  Does not change during device operation.
  Can be reduced by high T anneal after oxidation.

## Slide 25: Charge in SiO2
Si/SiO2 defects: 109-1011 cm-2
Si surface atoms 1015 cm-2
4 main kinds of defects:
Qit= interface trapped charge
  Located at the interface
  Probably related to incompletely oxidized Si end/or dangling bonds
  Can be positive/negative or neutral
  Traps levels in the forbidden gap (usually near valence and conduction band).
  450°C H2 anneal is effective in reducing Qit denisty

## Slide 26: Charge in SiO2
Si/SiO2 defects: 109-1011 cm-2
Si surface atoms 1015 cm-2
4 main kinds of defects:
QM= mobile ionic charges
  Attributed to alkali ions (Na, K, Li) as well as negative ions and heavy metals
  Less important if contamination is kept under control in clean room
  Cleaning furnace tubes with HCl helps preventing contamination.

## Slide 27: Charge in SiO2
Si/SiO2 defects: 109-1011 cm-2
Si surface atoms 1015 cm-2
4 main kinds of defects:
Qot= oxide trapped charge
  Located anywhere in the oxide
  Broken Si-O bonds
  Result in traps in the bulk oxide
  Usually due to ionizing radiation or damaging process steps (ion implantation, plasma etching…)

## Slide 28: CV characterization of SiO2

## Slide 29: CV characterization of SiO2
Qf presence:
Inversion is more difficult to obtain since a negative image charge is formed in the silicon.
C/V characteristic is shifted to the left
Qm shows a similar effect ( but of different amplitude since the position of the charge in the oxide is not fixed)
Qit presence:
Ef moves with respect to valence and conduction band sweeping the CV curve  interface traps are filled and emptied  CV curve is “stretched”
A zone: int. states near conduction band
B zone: int. states near mid band gap
C zone: inte. States near valence band

## Slide 30: CV characterization of SiO2
Interface state density
Quasi-static method:
Distortion of LF curve with respect to HF curve is due to interface states
Other commonly measured paramaters:
  Breakdown voltage
  Charge to breakdown by TDDB (Time dependent dielectric breakdown) test
  Mobile charge estimation by BTS ( Bias Temperature Stress)

## Slide 31: Nitridation
Nitridation is mainly utilized to form a barrier to the diffusion of B from the control gate into the silicon substrate and to improve thin oxide electrical quality (Qbd, resistance to trapping and to the generation of interface states after hot electron stress)
Most common nitridation techniques consist in annealing treatments made after the thermal oxidation step, at high or medium temperature with NH3 , N2O, NO by furnace or RTP.
Nitridation by NO is becoming the leading technology.
Best results are obtained by the formation of a N rich layer at theSi/SiO2 interface, avoiding N incorporation in the oxide bulk

## Slide 32: Silicon oxidation equipments/techniques
Furnace
Vertical furnaces
  Wafers batches (up to 100) are inserted in a quartz tube.
  Reactant gases are flown in the furnace
  Desired T is reached by resistive heating

## Slide 33: RTO
Rapid thermal oxidation (RTO) is increasingly used in the growth of
thin, high-quality dielectric layers and to reduce the thermal budget.
Kinetics may be influenced by both thermally and photon induced processes
Activation energies are usually different from conventional growth techniques ones

## Slide 34: Advanced oxidation techniques
Radical oxidation (e.g. ISSG by Applied Materials):
  H2 and O2 are directly inserted in a RTO chamber
  Water and radicals (O, OH) are formed
  Reactive species and low pressures guarantee high quality oxides

## Slide 35: Silicon oxidation equipments
Plasma oxidation: e.g. SPA
Low thermal budget (300/500 °C)
Ultra thin, high quality oxides

## Slide 36: Alternative gate oxides
Dielectric constant
A practical SiO2 thickness to avoid gate tunnelling: 0.8 nm
If xox cannot be scaled higher k
Requisites for an alternative gate dielectric:
  High k
  Band offset with respect to Si >1eV, band gap >4/5 eV
  Thermodynamically stable in contact with Silicon
  Compatible with IC process flow

## Slide 37: Alternative gate oxides

## Slide 38: Silicon oxide colour chart
http://www.ee.byu.edu/cleanroom/color_chart.phtml