## Slide 1: Etching

## Slide 2: Introduction
After thin films are deposited, they are usually removed from the wafer surface to form the desired pattern.
Sometimes the silicon substrates is patterned too
After patterning photo resist and/or hard masks are etched away form the entire wafer
Etching can be performed in wet or dry (plasma) environment

## Slide 3: Etch parameters/requirements
Etch rate
  Amount of material removed per unit time
Selectivity
  Ratio of the etch rates of different materials
  Mask and materials underneath the film to be patterned must be preserved
Anisotropy
  Vertical etch rate/horizontal etch rate
  A certain degree of anisotropy is often needed: features patterned on photo resist must be reproduced into the underlying film
  Structures profile shape must be accurately controlled.
Uniformity

## Slide 4: Wet etching
Wet chemical etchants are used
Wafers are immersed into baths or sprayed with chemicals

## Slide 5: Wet etching
First method used in microelectronics, now widely used especially to remove hard masks, photo resist and dry etching by products.
Pros
  Very high selectivity
  High uniformity and etch rate control
Cons
  No anisotropy (except for crystalline orientation dependent silicon etch)

## Slide 6: Etching Chemistries
 | Designation | Chemical Constituent
SiO2 | Hydrofluoric acid | HF:H2O
 | BOE,BHF | HF:NH4F:H2O
 | SC1 | NH4OH:H2O2H2O
Si3N4 | Hydrofluoric acid | HF:H2O
 | (orto-)phosphoric acid | H3PO4
Organics | Piranha,SPM | H2SO4:H2O2
 | SOM | H2SO4:O3
 | Ozonized DIW | DIW:O3
Si | Nitric:HF | HF:HNO3
 | Silicon etch | HF:HNO3: H2SO4: H3PO4
 | Tetramethylammonium-hydroxide | TMAH
 | Ammonium hydroxide | NH4OH
 | Potassium hydroxide | KOH
 | Hydrazine/water | N2H4:H2O
W | Peroxide | H2O2
 | SC1 | NH4OH:H2O2H2O
 | SC2 | HCl:H2O2:H2O
Al | SC2 | HCl:H2O2:H2O
 | SC1 | NH4OH:H2O2H2O
 | Designation | Chemical Constituent
Cu | Ozonized water | O3:H2O
 | SC2 | HCl:H2O2:H2O
Ti | SC1 | NH4OH:H2O2H2O
 | SC2 | HCl:H2O2:H2O
 | Hydrofluoric acid | HF:H2O
Co | SC2 | HCl:H2O2:H2O
 | Piranha,SPM | H2SO4:H2O2
Ni | Piranha,SPM | H2SO4:H2O2
Ta | Hydrofluoric acid | HF:H2O
 | Nitric:HF | HF:HNO3
TaN | Nitric:HF | HF:HNO3
Al2O3 | (orto-)phosphoric acid | H3PO4
 | Hydrofluoric acid | HF:H2O
HfO2 | Hydrofluoric acid | HF:H2O
 | Nitric:HF | HF:HNO3
ZrO2 | Hydrofluoric acid | HF:H2O
 | (orto-)phosphoric acid | H3PO4
 | Piranha,SPM | H2SO4:H2O2
 | Nitric:HF | HF:HNO3
Notes: Questo e’ un elenco di chimiche che si possono utilizzare per attaccare vari materiali. Ad esempio, si vede che l’ossido di silicio puo’ essere attaccato dall’acido fluoridrico, oppure da acido fluoridrico tamponato con ammonio fluoruro. Il nitruro puo’ attaccare con l’acido fluoridrico oppure con l’acido fosforico.

## Slide 7: Advanced celaning/wet etching
Advanced wet processes challenges:
  Particle removal efficiency
    Foam and bubble cleaning (CO2 or Nitrogen)
    Nozzle spray celaning
    Laser generated bubbles
    Non newtonian fluids [0 shear stress]
    Micro machined nano-tweezers (mask fabrication)
  Pattern collapse
    HF vapor
    Plasma + sublimation
    Cryogenic aerosol (N2)
    Super-critical CO2 [0 surface tension]

## Slide 8: Plasma etching
A plasma is used to etch the desired material:
  Both chemical reactions and ionic bombardment contribute to film removal.
Pros
  High anisotropy
  Profile shape controllability
Cons
  Contamination
  Damage
  Loading and memory effects
  Etch by-products to be removed

## Slide 9: Plasma etching
Typical RF-powered plasma etch systems look just like PECVD or sputtering systems.
Both chemical (highly reactive) species and ionic (very directional) species typically play a role.
VP is positive to equalize electron and ion fluxes.
Smaller electrode has higher fields to maintain current continuity (higher RF current density).

## Slide 10: Plasma etching basic mechanisms
Etching gases include halide-containing species such as CF4, SiF6, Cl2, and HBr, plus additives such as O2, H2 and Ar. O2 by itself is used to etch photoresist.
Pressure = 1 mtorr to 1 torr.
Typically there are about 1015 cm-3 neutral species (1 to 10% of which may be free radicals) and 108-1012 cm-3 ions and electrons.
In standard plasma systems, the plasma density is closely coupled to the ion energy (as determined by the sheath voltage). Increasing the power increases both.

## Slide 11: Plasma etching basic mechanisms
Chemical etching
Gas phase etchants are formed in the plasma (often, very reactive radicals)
Arrival angle distribution is uniform (cosnq with n=1)
Low sticking coefficient Ss
Since the etch is purely chemical, it’s also isotropic
High selectivity
Es.
e-+CF4  CF3+F+e-
4F+Si(s)  SiF4

## Slide 12: Plasma etching basic mechanisms
Physical etching (sputtering)
Sputtering yields are usually low ( one atom/incident ion)
Sputtering yield also depends on arrival angle (see figure)  faceting
Directional arrival angle distribution, Sc=1  anisotropic etching
Note: some chemical reaction can also occur during ion bombardment if ionized species are reactive.
Incident angle
Normalized Sputtering yield, Y
0
1
2
3
0
1
0
2
0
3
0
4
0
5
0
6
0
7
0
8
0
9
0
0
1
2
3

## Slide 13: Plasma etching basic mechanisms
Ion enhanced etching
Ion bombardment and chemical etching seem to work in a synergetic way:
Resulting etch rate is higher than the sum of single etch rates
Anisotropy is very high
Unexplained mechanism:
  Chemical reaction enhancement (e.g. bonds breaking)
  Inhibitor removal (see next slide)

## Slide 14: Plasma etching basic mechanisms
Ion enhanced inhibitor etching
A inhibitor or a “passivation” layer is formed and removed by ion bombardment (but stays on structures sidewalls)

## Slide 15: Etching tools
Barrel etcher
  Plasma is kept separated by wafers  no ion bombardment
    High selectivity
    No anisotropy
  Not used in modern IC manufacturing
  Downstream plasma concept still used for resist ashing

## Slide 16: Etching tools
Parallel plate etcher
  Very similar to PE-CVD chambers we already described.
  Can be operated in:
    Plasma mode: symmetrical electrodes lead to poor ion bombardment, small sheath voltage drop at wafer surface.
    RIE (Reactive Ion Etching) mode: asymmetric electrodes guarantee enhanced ion bombardment
NOTE: All the etching systems in modern IC manufacturing are SINGLE WAFER TOOLS

## Slide 17: Etching tools
High density plasma systems
  Plasma density and ion energy control are “decoupled”
    Bottom (wafer holding) electrode is controlled by an RF source
    Plasma is ignited by ECR (Electron Cyclotron Resonance) or ICP (Inductively Coupled Plasma) systems
    Can be operated in th 1-10 mTorr range
    High ion density and relatively low ion bombardment can be achieved simultaneously

## Slide 18: Etching tools
Sputter etching and Ion milling
  In sputter etching, only the sputtering component is exploited.
  In Ion Milling a confined plasma is used to generate ions (es. Ar+), grids are then used to accelerate ions toward the target (electron are eventually used to neutralize the beam). The Ar beam can also be focused ( used for mask repairing and TEM sample preparation).

## Slide 19: Summary of etching tools/techniques

## Slide 20: End point detection
Species in plasma are excited and emit photons at specific wavelengths.
Using Optical Emission Spectroscopy, a specific wavelength relative to a reactant or to a reaction product can be tracked.

## Slide 21: Plasma etching process “knobs”
Power.
  RIE: 0.1/5 Wcm-2 , ion energy =10/700 eV
  HDP: 0.1/3 Wcm-2, ion energy = 10/500 eV
Pressure
  RIE: 10/100 mTorr
  HDP: 1/10 mTorr
Gas species, flow rate and distribution
Wafer and chamber temperature

## Slide 22: Etch rate dependence on “knobs”
Etch rate dependence on power, pressure, flow rate an T is quite complicated, and can strongly depend on etch systems design. Generally speaking:
  Etch rate obviously depends on gas species
  Increasing power increases etch rate (in HDP systems ion bombardment can also be independently controlled)
  Increasing pressure decreases ion density, but increases chemical flux  etch rate dependence on pressure is not easily predictable
  Flow rate has a minor impact on etch rate ( can be increased to supply more reactant species, but high flow rate can decrease too much the residence time)

## Slide 23: Etch profile dependence on “knobs”
Etch profile can be controlled by:
  Increasing/decreasing ion bombardment ( power )
  Using different etchant gases, to control by-product formation and passivation layers deposition/removal process

## Slide 24: Plasma etching issues
Loading effects
  Etch rate dependence on local plasma density
Micro-loading effect
  Structures with different mask openings or aspect ratios are etched with different etch rates
Can be due to:
Depletion or trapping of reactant species
Distortion of ion paths due to charging
Shadowing effects

## Slide 25: Plasma etching issues
Micro trenching (ion physical deflection)
Resist re-sputtering
Ion trajectory distortion due to resist charging

## Slide 26: Plasma etching issues
Radiation damage
  Wafer surface can suffer from displaced atoms and implanted species such as H and C.
Active oxides plasma damage (antenna effect)
Substrate doping dependence

## Slide 28: Plasma etching chemistries
Silicon oxide
Fluorine based chemistries are used; F radicals are very reactive
Gases like NF3,SF6,CF4 result in very isotropic etching, silicon selectivity is also poor.
Adding O2 to CF4 increases the density of F radicals ( reducing recombination of C and F).
Fluorine-poor chemistries like CHF3, C3F8 or C2F6 can be used to reduce isotropy . Increasing C/F ratio also increases polymer deposition and profile control

## Slide 29: Plasma etching chemistries
Silicon and poly-silicon
Due to SiF4 volatility, F-based chemistries can be used to etch Si as well.
Problems:
SiO2 selectivity
Anisotropy
Adding O2 to CF4 can increase oxide selectivity ( Si etch is enhanced much more than SiO2 etch)
Halogen gases are used to increase both selectivity and anisotropy (less chemical component)
Cl2 and HBr are the most commonly used gases. Adding O2 can activate inhibitor deposition, allowing profile control

## Slide 30: Plasma etching chemistries
Aluminum
  Ion bombardment/sputtering to get rid of native Al2O3
  Cl based chemistries to increase volatility of by-products
  Strong inhibitor usage to avoid lateral erosion
  Higher temperatures to allow for evaporation of Cu based by-products.
  Post etch treatments needed to avoid Cl reacting with atmosphere H2O  HCl formation and Al corrosion,

## Slide 31: Etching models
Simple empirical models have to be derived for dry etching, since most of basic mechanisms are still not understood.
As usual, we should model the arrival angle distribution for each point of the wafer.
n=1 for neutral chemical species, n=10 to 80 for ions
We will also use the sticking coefficient concept. With Sc=1 for ionic species, and very low for neutral chemicals, that “bounce” around

## Slide 32: Etching models
Simple linear model
The simplest way to proceed is to imagine that sputtering and chemical reaction act independently. We can thus write
Kf is a reaction rate constant, Ki is the effective sputtering yield, depending both on incident angle and ion energy.
N is the density of the film to be etched.
Micro-loading effects can be, for example, simulated

## Slide 33: Etching models
Ion enhanced etching model:
  Neutral species are adsorbed to the surface to chemically react with the film
  Byproducts are removed by ion bombardment
  Number of species adsorbed is proportional to number of sites available (i.e. how many sites are free from by-products)
  Number of by-products removed is proportional to ion flux
Where 1-q is the fraction of available sites. Assuming steady state condition:

## Slide 34: Etching models
If either flux is zero, the overall etch rate is zero since both are required to etch the material.
Etch rate saturates when one component gets too large relative to the other (limited by slower of two series processes).
General approach with broad applicability. (But does not account for independently formed inhibitor layer mechanism, and does not model excess inhibitor formation.)